Aluminum Alloys

The applications for aluminum alloys are almost limitless.  Choosing an Aluminum alloy for a particular application depends on many factors.  Our Sales Staff can help you with this decision.

Some considerations that should be taken into account are:

- Foundry characteristics for the casting process that will be used;

- Required mechanical and other properties for the service intended;

- Mechanical properties over the service life;

- Corrosion resistance for the application;

- Machinability, pressure tightness and finishability, if necessary;

Another consideration that should be taken into account is the finished cost of the part.  The following among many other variables can directly affect the cost:

- The alloy chosen and the technical requirements of casting that alloy;

- Quantity of castings to be produced;

- Process used;

- Complexity of the shape of the part;

- The tooling used for producing the molds;

- Dimensional tolerances required;

- Inspection and quality standards required

- Common Alloys we pour at Bergstrom Foundry:

|  | Typical Mechanical Properties |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Tensile Strength | Yield Strength | Elongation | Hardness |
|  |  | psi | psi | % in 2" | (500 kg load) |
|  | 319 | 27,000 | 18,000 | 2 | 70 |
|  | 319-T6 | 36,000 | 24,000 | 2 | 80 |
|  | A356 | 23,000 | 12,000 | 6 | 70 |
|  | A356-T6 | 40,000 | 30,000 | 6 | 75 |
|  | 357.0 | 25,000 | 13,000 | 5 | - |
|  | 357-T7 | 46,000 | 36,000 | 3 | 85 |
|  | 535 | 40,000 | 20,000 | 13 | 70 |
|  | 705 | 30,000 | 17,000 | 5 | - |
|  | 713 | 32,000 | 22,000 | 3 | 75 |